# INCOMING MATERIAL

# QC INSPECTION MATRIX

Flexible Packaging Plant — All Raw Material Groups

DOCUMENT PURPOSE

This document defines all incoming QC inspection tests required for every raw material group used in the plant.

Please verify:

(a) that the tests listed are complete and correct for your process,

(b) that the specification limits align with your supplier agreements,

(c) that the frequencies reflect your operational capacity.

DOCUMENT STRUCTURE

Section 1  —  Key Principles and Sampling Rules

Section 2  —  Legend (Level, Frequency, Who)

Sections 3–17  —  Test matrix per material group (15 groups)

1. Key Principles — Incoming QC Philosophy

The fundamental rule for incoming inspection is:

Visual inspection = every roll / every pallet.  Lab tests = every lot (one composite sample).

What incoming QC must do:

Make a fast ACCEPT or REJECT decision before materials enter the production warehouse

Verify supplier compliance against Certificate of Analysis (CoA) and Purchase Order

Check the parameters that are critical to your process — not full laboratory characterization

What incoming QC does NOT do:

Full mechanical characterization (tensile, elongation, BCT) — this belongs to supplier qualification

OTR / WVTR barrier testing on every lot of transparent films — CoA acceptance is standard practice

Re-test every parameter declared on the CoA — CoA verification plus key functional checks is correct

1.1  Sampling Rules by Frequency

| FREQUENCY | TESTED BY | TESTS COVERED | WHEN / TRIGGER |
| --- | --- | --- | --- |
| Every Roll | Operator | Visual, width, weight, core ID, foil pinholes | All film/foil rolls at goods receipt dock |
| Every 5th Roll | QC Technician | Surface dyne level (all plastic films), foil wettability | Quick dyne pen test |
| 3 Rolls per Lot | QC Technician | Thickness profile (first, middle, last roll) | Catches within-lot variation |
| Every Lot | QC Lab | MFI, density, moisture, COF, seal tests, viscosity, KF water | Composite sample from 3 bags/drums |
| Every Pallet / Drum / Bag | Operator | Packaging integrity, labelling, visual of containers | Before materials enter warehouse |
| Every Lot (5 pcs AQL) | QC Technician | Core dimensions, carton dimensions | Not every piece — risk-based sample |
| Supplier Qualification | QC Lab | OTR, WVTR, tensile, BCT, puncture resistance | Once per new supplier — not routine incoming |
| If Issues Only | QC Lab | Bulk density, residue, haze, mechanical tests | Triggered by production complaint or dispute |

1.2  Supplier Approval Levels

Sampling frequency should be adjusted based on supplier maturity:

New supplier (first 3 months): test every lot, all Level 1 tests. Build your own data.

Approved supplier (stable history, CoA consistent): standard frequencies as shown in this document.

Problematic supplier (recent deviations): increase to every lot for all tests until root cause is closed.

MANDATORY tests (regardless of supplier status): Foil pinhole count (every roll) | Flash point label check for solvents (every drum) | ISPM-15 stamp on wooden pallets (every pallet) | Product code match for tapes (every roll). These are non-negotiable.

2. Legend — How to Read the Test Tables

| CODE | LABEL | MEANING |
| --- | --- | --- |
| L1 | Level 1 — Required | Every lot or every roll per rule. Must be done before material is accepted into production. |
| L2 | Level 2 — Periodic | Quarterly, supplier qualification, or if production issues arise. Not done on every receipt. |
| COND | Conditional | Applies to tagged sub-type only (e.g. HS grades, Metalized grades, Shrink grades). Skip if not applicable. |
| WHO | ROLE | SCOPE |
| Operator | Operator | Goods receipt dock. No lab equipment. Visual, dimensional, packaging checks. |
| QC Technician | QC Technician | Portable instruments. Dyne pens, callipers, micrometer, moisture analyser. |
| QC Lab | QC Lab | Lab equipment required. MFI tester, COF tester, seal strength, KF titration. |

Conditional tests (▶) are pre-tagged with the applicable sub-type in brackets, e.g. [HS GRADES ONLY] or [METALIZED ONLY]. Skip these rows if the received material is not that sub-type. All other Level 1 tests apply regardless of sub-type.

3. RESINS

HDPE / LDPE / LLDPE / mLLDPE / Random PP

8 Level 1 tests  |  3 Level 2 tests  |  11 total

SAMPLING RULE: Lab tests on 1 composite sample per lot (mix pellets from 3 bags). Visual on every pallet. MFI condition: PE @ 190°C / 2.16 kg  |  PP @ 230°C / 2.16 kg (ASTM D1238).

| LV | TEST NAME | METHOD | UNIT | SPEC / LIMIT & NOTES | FREQUENCY | TESTED BY |
| --- | --- | --- | --- | --- | --- | --- |
| L1 | Packaging Integrity — Bags / Octabin | Visual | — | Inner liner sealed; outer bag intact; no tears, moisture ingress or pest damage | Every Pallet | Operator |
| L1 | Label Check — Grade, Supplier, Batch | vs. Purchase Order | Pass/Fail | Grade code, supplier name and batch number on each bag must match PO exactly | Every Lot | Operator |
| L1 | Pellet Appearance | Visual — 100 g spread on tray | — | Uniform shape and natural colour. Zero black specks, gels, yellowing or agglomerates | Every Lot (1 bag) | Operator |
| L1 | Foreign Contamination | Visual — 100 g spread on tray | — | Zero tolerance. Any foreign material, insects or cross-contamination = REJECT lot | Every Lot (1 bag) | Operator |
| L1 | Melt Flow Index (MFI) | ASTM D1238 / ISO 1133 | g/10min | Within ±10% of CoA declared value. Composite sample from 3 bags | Every Lot | QC Lab |
| L1 | Density | ASTM D792 / ISO 1183-A | g/cm³ | Within ±0.003 g/cm³ of CoA declared value | Every Lot | QC Lab |
| L1 | Moisture Content | Moisture Analyzer / ASTM D6980 | % | Max: 0.05 ¦ ≤ 0.05% — excess moisture causes bubbles and surface defects in blown film | Every Lot | QC Lab |
| L1 | CoA Verification — All Parameters | vs. Supplier CoA | Pass/Fail | Check all declared values (MFI, density, additive package) against CoA. Sign and file | Every Lot | QC Technician |
| L2 | Bulk Density | ISO 60 | kg/m³ | Test only if volumetric hopper dosing or feeding inconsistency is reported | If Issues | QC Lab |
| L2 | Odor | Sensory evaluation | — | Characteristic resin odor only. Burnt / chemical / foreign odor = REJECT | New Supplier | QC Technician |
| L2 | Pellet Size Uniformity | Sieve analysis | — | Fines < 2 mm must be < 5% by weight. Only check if extrusion screen pack blocking | If Issues | QC Lab |

4. BOPP FILM

Standard / Heat-Sealable (HS) / Metalized / Matt / Pearlised / Label / Shrink

16 Level 1 tests  |  3 Level 2 tests  |  19 total

SAMPLING RULE: Visual on every roll (operator at dock). Dyne level every 5th roll. Thickness on 3 rolls per lot (first, middle, last). Lab tests on lot basis.

| LV | TEST NAME | METHOD | UNIT | SPEC / LIMIT & NOTES | FREQUENCY | TESTED BY |
| --- | --- | --- | --- | --- | --- | --- |
| L1 | Visual — Surface Defects | Visual + light table | — | Gels, holes, scratches, streaks, fish-eyes, contamination, uneven corona = REJECT roll | Every Roll | Operator |
| L1 | Visual — Roll Defects | Visual | — | Telescoping, soft/hard edges, starring, cinching, winding defects = REJECT roll | Every Roll | Operator |
| L1 | Width | Steel tape | mm | Within ±2 mm of order specification | Every Roll | Operator |
| L1 | Roll Weight — Net | Calibrated scale | kg | Within ±2% of declared net weight (deduct core and wrapper) | Every Roll | Operator |
| L1 | Core Inner Diameter | Vernier caliper | mm | 76 mm or 152 mm per order spec ± 0.5 mm | Every Roll | Operator |
| L1 | Surface Dyne Level — Print Side | ASTM D2578 — dyne pens | mN/m | Min: 38 ¦ ≥ 38 mN/m all grades ¦ ≥ 40 mN/m high-resolution print. CRITICAL for ink adhesion | Every 5th Roll | QC Technician |
| L1 | Thickness — Average (5-point) | ASTM D374 / ISO 4591 | µm | Within ±1.0 µm of nominal. Measure at 5 equidistant points across width | 3 Rolls per Lot | QC Technician |
| L1 | Thickness — Variation (Max–Min) | ASTM D374 / ISO 4591 | µm | Max–Min across width ≤ 10% of nominal thickness | 3 Rolls per Lot | QC Technician |
| L1 | COF — Static (Film-to-Film) | ASTM D1894 | — | Max: 0.35 ¦ ≤ 0.35 — critical for VFFS and auto-packaging lines. Test both surfaces | Every Lot | QC Lab |
| L1 | Shrinkage — MD (120°C / 5 min) | ASTM D2732 | % | Max: 3.0 ¦ ≤ 3.0% MD — excess shrinkage causes tunneling in laminated structures | Every Lot | QC Lab |
| L1 | Shrinkage — TD (120°C / 5 min) | ASTM D2732 | % | Max: 1.5 ¦ ≤ 1.5% TD — dimensional stability in transverse direction | Every Lot | QC Lab |
| L1 | CoA Verification | vs. Supplier CoA | Pass/Fail | Verify thickness, dyne, COF, shrinkage, density against CoA. Sign and file | Every Lot | QC Technician |
| COND | ▶ [HS] Seal Initiation Temp (SIT) | Gradient bar sealer | °C | [HS GRADES ONLY] Verify SIT matches CoA declared range. Typical 90–110°C | Every Lot | QC Lab |
| COND | ▶ [HS] Seal Strength | ASTM F88 — T-peel | N/15mm | Min: 150 ¦ [HS GRADES ONLY] ≥ 150 N/15mm at optimal seal temp. 24h conditioning at 23°C | Every Lot | QC Lab |
| COND | ▶ [MET] Optical Density (OD) | Densitometer | OD | 2.0 – 3.0 ¦ [METALIZED ONLY] OD 2.0–3.0. Low OD = insufficient barrier or metalizing defect | Every Lot | QC Lab |
| COND | ▶ [SHRINK] Shrinkage MD (120°C) | ASTM D2732 | % | 40 – 60 ¦ [SHRINK ONLY] 40–60% MD — verify against sleeve geometry requirements | Every Lot | QC Lab |
| COND | ▶ [MET] OTR — Periodic Batch Check | ASTM D3985 | cc/m²/day | [METALIZED ONLY] Test 1 roll per lot for first 3 lots from new batch; then every 5th | Every 5th Lot | QC Lab |
| L2 | Tensile Strength MD / TD | ASTM D882 | MPa | Per TDS — supplier qualification or dispute only. NOT routine incoming | Supplier Qualification | QC Lab |
| L2 | Haze (Transparent grades) | ASTM D1003 | % | Only for transparency-critical jobs (window patch, display packaging) | If Issues | QC Lab |

5. CPP FILM

Cast Polypropylene — Heat-Sealable (HS) and Metalized

13 Level 1 tests  |  1 Level 2 tests  |  14 total

CPP is a sealant / inner layer. Seal performance tests are MANDATORY Level 1 — not optional. Visual every roll; seal and SIT tests every lot on 2 sampled rolls.

| LV | TEST NAME | METHOD | UNIT | SPEC / LIMIT & NOTES | FREQUENCY | TESTED BY |
| --- | --- | --- | --- | --- | --- | --- |
| L1 | Visual — Surface Defects | Visual + light table | — | Gels, holes, haze bands, streaks, edge damage, contamination = REJECT roll | Every Roll | Operator |
| L1 | Visual — Roll Defects | Visual | — | Telescoping, soft/hard edges, blocking, cinching = REJECT roll | Every Roll | Operator |
| L1 | Width | Steel tape | mm | Within ±2 mm of order specification | Every Roll | Operator |
| L1 | Roll Weight — Net | Calibrated scale | kg | Within ±2% of declared net weight | Every Roll | Operator |
| L1 | Core Inner Diameter | Vernier caliper | mm | 76 mm or 152 mm ± 0.5 mm per order spec | Every Roll | Operator |
| L1 | Surface Dyne Level | ASTM D2578 — dyne pens | mN/m | Min: 38 ¦ ≥ 38 mN/m sealant side; ≥ 40 mN/m print side if applicable | Every 5th Roll | QC Technician |
| L1 | Thickness — Average (5-point) | ASTM D374 / ISO 4591 | µm | Within ±1.5 µm of nominal. CPP typically 20–50 µm | 3 Rolls per Lot | QC Technician |
| L1 | Seal Initiation Temp (SIT) | Gradient bar sealer | °C | CRITICAL — SIT must match lamination line settings. Typical: 100–130°C per TDS | Every Lot | QC Lab |
| L1 | Seal Strength (CPP-to-CPP) | ASTM F88 — T-peel | N/15mm | Min: 200 ¦ ≥ 200 N/15mm at optimal seal conditions. 24h conditioning at 23°C/50%RH | Every Lot | QC Lab |
| L1 | Hot Tack Strength | ASTM F1921 | N/15mm | Min: 100 ¦ ≥ 100 N/15mm — critical for VFFS high-speed packaging lines | Every Lot | QC Lab |
| L1 | COF — Static (Sealant Side) | ASTM D1894 | — | Max: 0.40 ¦ ≤ 0.40 — excess COF causes jams on auto-packers | Every Lot | QC Lab |
| L1 | CoA Verification | vs. Supplier CoA | Pass/Fail | Thickness, dyne, SIT, seal strength — all verified | Every Lot | QC Technician |
| COND | ▶ [MET] Optical Density (OD) | Densitometer | OD | 2.0 – 3.0 ¦ [METALIZED ONLY] OD 2.0–3.0 — barrier performance | Every Lot | QC Lab |
| L2 | Tensile Strength MD / TD | ASTM D882 | MPa | Per TDS — audit or troubleshooting only. Not routine incoming | Supplier Qualification | QC Lab |

6. PET FILM

Transparent (Chem. Treated) / Metalized / Matt / Shrink (PETG) / Twist

15 Level 1 tests  |  2 Level 2 tests  |  17 total

PETG shrink has different density (1.27–1.33 g/cm³) vs standard BOPET (1.40 g/cm³) — verify correct grade is received. OTR/WVTR accepted on CoA for transparent grades; test metalized grades periodically.

| LV | TEST NAME | METHOD | UNIT | SPEC / LIMIT & NOTES | FREQUENCY | TESTED BY |
| --- | --- | --- | --- | --- | --- | --- |
| L1 | Visual — Surface Defects | Visual + light table | — | Scratches, gels, haze spots, pit marks, contamination, curl = REJECT roll | Every Roll | Operator |
| L1 | Visual — Roll Defects | Visual | — | Telescoping, soft edges, starring, blocking, embossing lines = REJECT roll | Every Roll | Operator |
| L1 | Width | Steel tape | mm | Within ±2 mm of order specification | Every Roll | Operator |
| L1 | Roll Weight — Net | Calibrated scale | kg | Within ±2% of declared net weight | Every Roll | Operator |
| L1 | Core Inner Diameter | Vernier caliper | mm | 76 mm or 152 mm ± 0.5 mm | Every Roll | Operator |
| L1 | Surface Dyne Level — Bond Side | ASTM D2578 — dyne pens | mN/m | Min: 44 ¦ ≥ 44 mN/m on chem-treated side. CRITICAL for ink and adhesive bond quality | Every 5th Roll | QC Technician |
| L1 | Thickness — Average (5-point) | ASTM D374 / ISO 4591 | µm | Within ±0.5 µm of nominal. PET typically 10–23 µm — tight tolerance | 3 Rolls per Lot | QC Technician |
| L1 | COF — Static | ASTM D1894 | — | Max: 0.50 ¦ ≤ 0.50 — PET has higher natural COF than BOPP. Check film-to-film | Every Lot | QC Lab |
| L1 | Haze (Transparent grades) | ASTM D1003 | % | Max: 2.0 ¦ ≤ 2.0% for transparent grades. Clarity-critical for retort pouches | Every Lot | QC Lab |
| L1 | CoA Verification | vs. Supplier CoA | Pass/Fail | Thickness, dyne, COF, density, shrinkage — all verified | Every Lot | QC Technician |
| COND | ▶ [MET] Optical Density (OD) | Densitometer | OD | 2.2 – 3.5 ¦ [METALIZED] OD 2.2–3.5 per application spec. Low OD = barrier failure | Every Lot | QC Lab |
| COND | ▶ [MET] OTR — Periodic Check | ASTM D3985 | cc/m²/day | [METALIZED] Test 1 roll per lot for first 3 lots from new batch; every 5th lot after | Every 5th Lot | QC Lab |
| COND | ▶ [PETG] Shrinkage MD (90°C / 10 sec) | ASTM D2732 — hot water bath | % | 65 – 78 ¦ [PETG SHRINK] 65–78% MD shrinkage — verify against sleeve print geometry | Every Lot | QC Lab |
| COND | ▶ [PETG] Shrinkage TD (90°C / 10 sec) | ASTM D2732 — hot water bath | % | Max: 5.0 ¦ [PETG SHRINK] ≤ 5% TD — minimal transverse shrinkage | Every Lot | QC Lab |
| COND | ▶ [PETG] Density Check | ASTM D792 | g/cm³ | 1.27 – 1.33 ¦ [PETG SHRINK] 1.27–1.33. Standard BOPET is 1.40 — wrong grade if ≥ 1.38 | Every Lot | QC Lab |
| L2 | OTR / WVTR — Standard PET | vs. Supplier CoA | cc/m²/day | Accept CoA for standard transparent PET. Lab test only for qualification or dispute | Supplier Qualification | QC Lab |
| L2 | Tensile Strength MD / TD | ASTM D882 | MPa | Per TDS — supplier qualification or dispute resolution only | Supplier Qualification | QC Lab |

7. PE FILM

LDPE Transparent Plain / PE Shrink (HDHC) / LDPE Lamination Roll

9 Level 1 tests  |  1 Level 2 tests  |  10 total

PE films are often sourced as semi-finished goods. Focus on dimensional and visual checks. Shrink tests mandatory for HDHC shrink grade only.

| LV | TEST NAME | METHOD | UNIT | SPEC / LIMIT & NOTES | FREQUENCY | TESTED BY |
| --- | --- | --- | --- | --- | --- | --- |
| L1 | Visual — Surface Defects | Visual + light table | — | Holes, gels, blocking, streaks, contamination, burn marks = REJECT roll | Every Roll | Operator |
| L1 | Visual — Roll Defects | Visual | — | Telescoping, blocking, soft edges, poor winding = REJECT roll | Every Roll | Operator |
| L1 | Width | Steel tape | mm | Within ±3 mm of order specification | Every Roll | Operator |
| L1 | Roll Weight — Net | Calibrated scale | kg | Within ±3% of declared net weight | Every Roll | Operator |
| L1 | Thickness — Average (5-point) | ASTM D374 / ISO 4591 | µm | Within ±2.0 µm of nominal. PE films typically 20–200 µm | 3 Rolls per Lot | QC Technician |
| L1 | COF — Static | ASTM D1894 | — | Max: 0.40 ¦ ≤ 0.40 — slip additive check. Test if auto-pack line feeding issues reported | Every Lot | QC Lab |
| L1 | CoA Verification | vs. Supplier CoA | Pass/Fail | Thickness, width, density — confirm all declared values | Every Lot | QC Technician |
| COND | ▶ [SHRINK] Shrinkage — MD (120°C) | ASTM D2732 | % | 40 – 70 ¦ [PE SHRINK ONLY] Verify shrink % matches application requirement per job spec | Every Lot | QC Lab |
| COND | ▶ [SHRINK] Shrinkage — TD (120°C) | ASTM D2732 | % | 40 – 70 ¦ [PE SHRINK ONLY] Balanced or preferential shrink per job specification | Every Lot | QC Lab |
| L2 | Tensile Strength — MD | ASTM D882 | N/15mm | Per TDS — troubleshooting only (film tearing on slitter or auto-packer) | If Issues | QC Lab |

8. PA FILM (NYLON)

Biaxially Oriented Polyamide (BOPA) — 15 µm standard

9 Level 1 tests  |  3 Level 2 tests  |  12 total

PA film is highly hygroscopic. Re-seal opened rolls immediately and condition 48 hours at 23°C / 50% RH before testing. OTR / WVTR accepted on CoA for routine receipts.

| LV | TEST NAME | METHOD | UNIT | SPEC / LIMIT & NOTES | FREQUENCY | TESTED BY |
| --- | --- | --- | --- | --- | --- | --- |
| L1 | Visual — Surface Defects | Visual + light table | — | Scratches, holes, haze variations, crystallinity spots, contamination = REJECT roll | Every Roll | Operator |
| L1 | Visual — Roll Defects | Visual | — | Telescoping, soft edges, blocking, moisture condensation marks = REJECT roll | Every Roll | Operator |
| L1 | Width | Steel tape | mm | Within ±2 mm of order spec | Every Roll | Operator |
| L1 | Roll Weight — Net | Calibrated scale | kg | Within ±2% of declared net weight | Every Roll | Operator |
| L1 | Packaging Seal — Moisture Protection | Visual | Pass/Fail | Roll must be in sealed moisture-proof bag. Open or compromised bag = REJECT | Every Roll | Operator |
| L1 | Thickness — Average (5-point) | ASTM D374 / ISO 4591 | µm | Within ±0.5 µm of nominal (15 µm). Very tight spec for PA | 3 Rolls per Lot | QC Technician |
| L1 | Surface Dyne Level | ASTM D2578 — dyne pens | mN/m | Min: 48 ¦ ≥ 48 mN/m — PA needs high surface energy for adhesive bond in lamination | Every 5th Roll | QC Technician |
| L1 | COF — Static | ASTM D1894 | — | Max: 0.45 ¦ ≤ 0.45 — PA naturally higher COF than BOPP. Test after conditioning | Every Lot | QC Lab |
| L1 | CoA Verification — OTR / WVTR / Tensile | vs. Supplier CoA | Pass/Fail | Verify OTR, WVTR, tensile, thickness on CoA. Accept CoA for routine receipt | Every Lot | QC Technician |
| L2 | OTR — Oxygen Barrier | ASTM D3985 | cc/m²/day | BOPA 15µm typical 30–50 cc/m²/day. Test during qualification or dispute only | Supplier Qualification | QC Lab |
| L2 | WVTR — Moisture Barrier | ASTM F1249 | g/m²/day | Per TDS. Test during qualification or if laminate barrier complaints received | Supplier Qualification | QC Lab |
| L2 | Puncture Resistance | ASTM F1306 | N | Key for retort / boil-in-bag. Per TDS — test during qualification only | Supplier Qualification | QC Lab |

9. PVC SHRINK FILM

Sleeve Labels & Tamper-Evidence Bands — 40 µm / 50 µm

8 Level 1 tests  |  2 Level 2 tests  |  10 total

Shrinkage profile is the critical commercial spec — test every lot. MD is the primary shrink direction. Density is fixed at 1.38 g/cm³ — verify correct grade received.

| LV | TEST NAME | METHOD | UNIT | SPEC / LIMIT & NOTES | FREQUENCY | TESTED BY |
| --- | --- | --- | --- | --- | --- | --- |
| L1 | Visual — Clarity & Blocking | Visual | — | No blocking between layers. High optical clarity required for label print quality | Every Roll | Operator |
| L1 | Visual — Roll Defects | Visual | — | No telescoping, soft edges, core slip, winding defects = REJECT roll | Every Roll | Operator |
| L1 | Width (lay-flat) | Steel tape | mm | Within ±2 mm of order spec. Lay-flat width = half of sleeve circumference | Every Roll | Operator |
| L1 | Roll Weight — Net | Calibrated scale | kg | Within ±2% of declared net weight | Every Roll | Operator |
| L1 | Thickness — Average (5-point) | ASTM D374 / ISO 4591 | µm | Within ±2 µm of nominal (40 or 50 µm). Thickness impacts shrinkage behavior | 3 Rolls per Lot | QC Technician |
| L1 | Shrinkage — MD (90°C / 10 sec) | ASTM D2732 — hot water bath | % | 45 – 55 ¦ MD 45–55% — primary shrink direction. Verify against job specification | Every Lot | QC Lab |
| L1 | Shrinkage — TD (90°C / 10 sec) | ASTM D2732 — hot water bath | % | Max: 5.0 ¦ ≤ 5% TD — minimal transverse shrinkage required for sleeve label geometry | Every Lot | QC Lab |
| L1 | CoA Verification | vs. Supplier CoA | Pass/Fail | Thickness, shrinkage MD/TD, density (1.38 g/cm³) — all verified | Every Lot | QC Technician |
| L2 | COF — Static | ASTM D1894 | — | Max: 0.40 ¦ ≤ 0.40 — test only if sleeve application machine jams are reported | If Issues | QC Lab |
| L2 | Tensile Strength | ASTM D882 | MPa | Per TDS — only during qualification or if film tearing on slitter | Supplier Qualification | QC Lab |

10. ALUMINIUM FOIL

7 µm / 8 µm / 9 µm Plain Foil — Alloy 8011-O (food) or 1235-O (pharma)

10 Level 1 tests  |  3 Level 2 tests  |  13 total

PINHOLE TESTING IS MANDATORY ON EVERY ROLL — NO EXCEPTIONS. Pinhole distribution is not uniform across a production run. One bad roll in a laminate batch destroys the entire finished goods lot.

| LV | TEST NAME | METHOD | UNIT | SPEC / LIMIT & NOTES | FREQUENCY | TESTED BY |
| --- | --- | --- | --- | --- | --- | --- |
| L1 | Visual — Surface Defects | Visual + strong backlight | — | Holes, tears, oil stains, scratch marks, wrinkles, oxidation (white powder) = REJECT | Every Roll | Operator |
| L1 | Visual — Roll Quality | Visual | — | Telescoping, bagging, core slip, lateral movement, moisture in packaging = REJECT | Every Roll | Operator |
| L1 | Width | Steel tape | mm | Within ±2 mm of order specification | Every Roll | Operator |
| L1 | Roll Weight — Net | Calibrated scale | kg | Within ±2% of declared net weight | Every Roll | Operator |
| L1 | PINHOLE COUNT — MANDATORY | Light table — 1 m² sample area | ph/m² | 7µm ≤ 30/m² ¦ 9µm ≤ 10/m² ¦ Any macroscopic hole visible to naked eye = REJECT ROLL | Every Roll | QC Technician |
| L1 | PINHOLE MAX SIZE | Light table / optical loupe | µm | Max: 40 ¦ ≤ 40 µm max pinhole size for food and pharma. Pinholes > 40 µm = REJECT roll | Every Roll | QC Technician |
| L1 | Thickness — Average (5-point) | ASTM B479 — micrometer | µm | 7µm: 6.7–7.3 ¦ 8µm: 7.7–8.3 ¦ 9µm: 8.7–9.3. Five points across width | 3 Rolls per Lot | QC Technician |
| L1 | Temper / Annealing — Bend Test | 90° manual fold test | Pass/Fail | O-temper (soft): no crack at 90° fold. H-temper cracks = wrong grade. REJECT if wrong | Every Lot | QC Technician |
| L1 | Wettability — Lamination Side | ASTM D2578 — dyne pens | mN/m | Min: 32 ¦ ≥ 32 mN/m — ensures adhesive bond in foil laminates. Quick 30-second test | Every 5th Roll | QC Technician |
| L1 | Alloy & Grade CoA Verification | vs. Supplier CoA and PO | Pass/Fail | Alloy (8011 or 1235), temper (O), thickness — all match CoA and PO | Every Lot | QC Technician |
| L2 | Tensile Strength | ASTM E8 | MPa | Per CoA — test during qualification or if laminate is delaminating | Supplier Qualification | QC Lab |
| L2 | Elongation at Break | ASTM E8 | % | O-temper typical 1–3%. Test during qualification or dispute only | Supplier Qualification | QC Lab |
| L2 | OTR / WVTR | ASTM D3985 / E96 | — | Pinhole-free foil = inherent zero barrier. Only test for pharma-grade qualification | Supplier Qualification | QC Lab |

11. PAPER & FOIL LAMINATES

Greaseproof / Kraft (SOS) / PE Coated / Rotocoat / Twist Wrap / Butter Foil

12 Level 1 tests  |  2 Level 2 tests  |  14 total

GSM is the primary incoming test for all paper grades — it drives cost and press settings. Greaseproof Kit Rating applies to GP grades only. Peel strength for foil laminate grades only.

| LV | TEST NAME | METHOD | UNIT | SPEC / LIMIT & NOTES | FREQUENCY | TESTED BY |
| --- | --- | --- | --- | --- | --- | --- |
| L1 | Visual — Surface Defects | Visual | — | Holes, stains, inclusions, uneven coating, edge damage, splice marks = REJECT roll | Every Roll | Operator |
| L1 | Visual — Roll Condition | Visual | — | Moisture staining, core damage, crushed rolls, outer wrap torn = REJECT roll | Every Roll | Operator |
| L1 | Width | Steel tape | mm | Within ±3 mm of order specification | Every Roll | Operator |
| L1 | Roll Weight — Net | Calibrated scale | kg | Within ±3% of declared net weight | Every Roll | Operator |
| L1 | Grammage — GSM | ISO 536 — cut and weigh | g/m² | Within ±5% of nominal. Cut 10×10 cm sample, weigh, multiply by 100 | Every Lot | QC Technician |
| L1 | Moisture Content | Moisture Analyzer / ASTM D644 | % | 3.0 – 8.0 ¦ 3–8% — balanced moisture critical. > 8% = blocking/mold risk. < 3% = brittleness | Every Lot | QC Lab |
| L1 | Thickness | Micrometer — 5-point | µm | Within ±5 µm of nominal. Verify consistency with GSM specification | Every Lot | QC Technician |
| L1 | CoA Verification | vs. Supplier CoA | Pass/Fail | GSM, moisture, grade — all values verified | Every Lot | QC Technician |
| COND | ▶ [GP] Greaseproof — Kit Rating | TAPPI T559 — Kit test | Kit # | 6 – 12 ¦ [GREASEPROOF ONLY] Kit 6–12. Higher = better grease barrier. Food minimum Kit 8 | Every Lot | QC Lab |
| COND | ▶ [PE-CTD] PE Coating Weight | Gravimetric — strip and weigh | g/m² | Min: 10 ¦ [PE COATED ONLY] ≥ 10 g/m² PE coating weight for moisture barrier | Every Lot | QC Lab |
| COND | ▶ [BUTTER FOIL] Peel Strength | ASTM F88 — T-peel 180° | N/15mm | Min: 100 ¦ [FOIL LAMINATE ONLY] Paper-to-foil peel ≥ 100 N/15mm — delamination check | Every Lot | QC Lab |
| COND | ▶ [BUTTER FOIL] Lacquer Uniformity | Visual — reflected light | — | [BUTTER FOIL ONLY] Uniform gloss, no bare spots, lacquer tears or blisters | Every Roll | Operator |
| L2 | Tensile Strength MD / CD | ISO 1924 | kN/m | Per TDS — only if runnability issues (web breaks on press or slitter) | If Issues | QC Lab |
| L2 | Tear Resistance MD / CD | ISO 1974 — Elmendorf | mN | Per TDS — qualification or complaint investigation only | Supplier Qualification | QC Lab |

12. ADHESIVES

Solvent-Based (2K) / Solvent-Less (2K) / Hot Melt

11 Level 1 tests  |  3 Level 2 tests  |  14 total

Test Component A and Component B SEPARATELY — mark which component in the header. Trial bond is MANDATORY for Solvent-Less adhesives: reactivity is batch-sensitive. A bad SL batch passing viscosity but failing bond destroys a production run.

| LV | TEST NAME | METHOD | UNIT | SPEC / LIMIT & NOTES | FREQUENCY | TESTED BY |
| --- | --- | --- | --- | --- | --- | --- |
| L1 | Packaging Integrity — Drum / Can | Visual | — | Drum sealed, no leaks, no crystallization at bung, correct GHS hazard labels | Every Drum | Operator |
| L1 | Label Check — Batch and Expiry | vs. Purchase Order / Label | Pass/Fail | Grade, batch code and expiry on drum match PO. ≥ 3 months shelf life remaining | Every Drum | Operator |
| L1 | Appearance — Color and Clarity | Visual | — | Clear to pale yellow. Turbidity, gelation, phase separation or dark color = REJECT | Every Lot (1 drum) | QC Technician |
| L1 | Odor | Sensory | — | Expected PU / solvent odor only. Rancid, ammonia or off-odor = REJECT | Every Lot (1 drum) | QC Technician |
| L1 | Viscosity — Component A | Brookfield / ISO 2555 @ 25°C | mPa·s | Within ±15% of CoA declared value. Significant deviation = contamination or aging | Every Lot | QC Lab |
| L1 | Viscosity — Component B (Hardener) | Brookfield / ISO 2555 @ 25°C | mPa·s | Within ±15% of CoA declared value at 25°C | Every Lot | QC Lab |
| L1 | Solids Content (Solvent-Based only) | ASTM D2369 — oven gravimetric | % | [SB ONLY] Within ±2% of CoA declared solids. Checks solvent loss over shelf life | Every Lot | QC Lab |
| L1 | Mix Ratio Check — by Weight | Calibrated scale | A:B | Weigh components at declared TDS ratio. Verify before production sign-off | Every Lot | QC Technician |
| L1 | Pot Life / Working Time | Time to viscosity doubling | min | Must match TDS declared pot life ±20%. Critical for solvent-less adhesives | Every Lot | QC Lab |
| L1 | CoA Verification | vs. Supplier CoA | Pass/Fail | Viscosity A&B, solids (SB), NCO content — all within tolerance. Sign and file | Every Lot | QC Technician |
| COND | ▶ [SL] Trial Bond — Peel Strength | ASTM F88 — 48h cure at 40°C | N/15mm | Min: 200 ¦ [SL ONLY] MANDATORY. ≥ 200 N/15mm after 48h cure. SL reactivity is batch-sensitive | Every Lot | QC Lab |
| COND | ▶ [HM] Softening Point | ASTM E28 — Ring and Ball | °C | [HOT MELT ONLY] Per TDS — verify grade matches application temperature window | New Supplier / Grade Change | QC Lab |
| COND | ▶ [HM] Open Time | Application test | sec | [HOT MELT ONLY] Per TDS — check during grade qualification only | Supplier Qualification | QC Lab |
| L2 | Density | Weight / volume | g/cm³ | Quick identity check — run only if identity of component is in doubt | If Issues | QC Lab |

13. MASTERBATCH & ADDITIVES

Color MB / Slip MB / Antiblock MB / UV Stabilizer MB / OBD MB / Antistatic MB / Process Aid MB

11 Level 1 tests  |  2 Level 2 tests  |  13 total

Composite sample: mix pellets from 3 bags before testing. Color ΔE test must be performed on blown film chip at declared dosing rate — not on raw pellets.

| LV | TEST NAME | METHOD | UNIT | SPEC / LIMIT & NOTES | FREQUENCY | TESTED BY |
| --- | --- | --- | --- | --- | --- | --- |
| L1 | Packaging Integrity and Label | Visual | — | Bag sealed, grade/colour/batch and dosing rate label intact, legible and matches PO | Every Bag | Operator |
| L1 | Pellet Appearance | Visual — 100 g spread on tray | — | Uniform shape, colour, size. No fines, agglomerates, contamination or colour spots | Every Lot (3 bags) | Operator |
| L1 | MFI | ASTM D1238 @ 190°C / 2.16 kg | g/10min | Within ±15% of CoA declared value. High deviation = wrong carrier or batch error | Every Lot | QC Lab |
| L1 | Moisture Content | Moisture Analyzer | % | Max: 0.10 ¦ ≤ 0.10% — MB absorbs moisture. Excess = bubbles and streaks in blown film | Every Lot | QC Lab |
| L1 | Carrier Resin Compatibility | vs. Process Resin Specification | Pass/Fail | PE carrier for PE process; PP carrier for PP process. Cross-carrier = haze and gels | Every Lot | QC Technician |
| L1 | CoA Verification | vs. Supplier CoA | Pass/Fail | MFI, pigment loading, carrier resin — all confirmed | Every Lot | QC Technician |
| COND | ▶ [COLOR] Color Match — ΔE | Spectrophotometer D65/10° | ΔE | Max: 1.0 ¦ [COLOR MB] ΔE ≤ 1.0 vs. approved reference chip. Test on blown film at std dosing | Every Lot | QC Lab |
| COND | ▶ [COLOR] Visual Match — D65 Lightbox | Visual under D65 illuminant | Pass/Fail | [COLOR MB] Match approved reference under D65 — check for metamerism under daylight | Every Lot | QC Technician |
| L1 | Dispersibility — Blown Film Trial | Film trial at standard dosing | — | No streaks, agglomerate trails, unmelted particles or fish-eyes in 1 m² sample | Every Lot | QC Lab |
| COND | ▶ [SLIP] COF — Blown Film at Dosing | ASTM D1894 | — | Max: 0.25 ¦ [SLIP MB] COF ≤ 0.25 in blown film at declared dosing rate | Every Lot | QC Lab |
| COND | ▶ [AB] Blocking Resistance | ASTM D3354 | N/m² | Max: 50 ¦ [ANTIBLOCK MB] ≤ 50 N/m² blocking force in blown film at standard dosing rate | Every Lot | QC Lab |
| COND | ▶ [UV] UV Absorbance | UV-Vis spectrophotometer | % | [UV MB] Test during supplier qualification only. Otherwise accept CoA | Supplier Qualification | QC Lab |
| COND | ▶ [OBD] Oxidation Induction Time (OIT) | DSC / ASTM D3895 | min | [OBD MB] Verify OIT shortened vs. control — qualification only | Supplier Qualification | QC Lab |

14. SOLVENTS & CHEMICALS

Ethyl Acetate (EA) / Methoxypropanol (PM) / Tetrahydrofuran (THF)

8 Level 1 tests  |  2 Level 2 tests  |  10 total

FLASH POINT is a MANDATORY safety and regulatory check — every lot, every drum label. Verifies storage class and ADR transport compliance. KF water content > 200 ppm causes adhesive hydrolysis and ink defects.

| LV | TEST NAME | METHOD | UNIT | SPEC / LIMIT & NOTES | FREQUENCY | TESTED BY |
| --- | --- | --- | --- | --- | --- | --- |
| L1 | Drum and Label Integrity | Visual | — | Drum sealed, no leaks, correct UN number, GHS hazard labels and ADR class label intact | Every Drum | Operator |
| L1 | Appearance | Visual | — | Clear, colourless liquid. Turbidity, colour or visible contamination = REJECT drum | Every Drum | Operator |
| L1 | Odor | Sensory | — | EA: ester (fruity). PM: mild ether. THF: strong cyclic ether. Foreign odor = REJECT | Every Drum | Operator |
| L1 | Flash Point — Label vs. Declared | vs. SDS / drum label | °C | EA: –4°C ¦ PM: +32°C ¦ THF: –14°C. Verify declared flash point matches SDS class | Every Drum | Operator |
| L1 | Purity / Assay — CoA Check | vs. Supplier CoA (GC purity) | % | Min: 99.0 ¦ ≥ 99.0% purity declared on CoA. Accept CoA for approved suppliers | Every Lot | QC Technician |
| L1 | Density @ 20°C | Hydrometer / pycnometer | g/cm³ | EA: 0.894–0.902 ¦ PM: 0.917–0.923 ¦ THF: 0.882–0.892. Identity and purity check | Every Lot (1 drum) | QC Technician |
| L1 | Water Content (KF Titration) | Karl Fischer / ASTM E1064 | ppm | Max: 200 ¦ ≤ 200 ppm water — CRITICAL. Excess water causes adhesive hydrolysis and ink defects | Every Lot | QC Lab |
| L1 | CoA Verification | vs. Supplier CoA | Pass/Fail | Purity, density, water content, flash point — all confirmed | Every Lot | QC Technician |
| L2 | Residue on Evaporation | ASTM D1353 | mg/100mL | Only if ink or adhesive quality complaint traces back to solvent contamination | If Issues | QC Lab |
| L2 | Refractive Index | ASTM D1218 — refractometer | n₂₀D | Quick identity check when identity is in doubt (wrong drum, unlabeled) | If Issues | QC Lab |

15. HEAT SEAL LACQUER

Heat Seal Lacquer (HSL) — Solvent-Based / Water-Based / Cold Seal Coating

10 Level 1 tests  |  1 Level 2 tests  |  11 total

All five performance tests (viscosity, solids, SIT, seal strength, hot tack) are Level 1 — HSL is a process-critical material. One bad batch can affect an entire day's coating run.

| LV | TEST NAME | METHOD | UNIT | SPEC / LIMIT & NOTES | FREQUENCY | TESTED BY |
| --- | --- | --- | --- | --- | --- | --- |
| L1 | Packaging and Label Integrity | Visual | — | Container sealed, no skin formation, correct grade/batch label, ≥ 3 months shelf life | Every Drum | Operator |
| L1 | Appearance — Color and Clarity | Visual | — | Clear to slight haze acceptable. Milky, cloudy or phase-separated = REJECT lot | Every Lot (1 drum) | QC Technician |
| L1 | Viscosity | Brookfield or Ford Cup #4 @ 25°C | mPa·s | Within ±15% of CoA. Controls coat weight and application uniformity | Every Lot | QC Lab |
| L1 | Solids Content | ASTM D2369 — oven gravimetric | % | Within ±2% of CoA declared solids. Directly controls coat weight and performance | Every Lot | QC Lab |
| L1 | Seal Initiation Temp (SIT) | Gradient bar sealer | °C | Must activate at declared SIT ±5°C. Verify against coating line settings | Every Lot | QC Lab |
| L1 | Seal Strength | ASTM F88 — T-peel | N/15mm | Min: 200 ¦ ≥ 200 N/15mm minimum at optimal seal conditions on target substrate | Every Lot | QC Lab |
| L1 | Hot Tack | ASTM F1921 | N/15mm | Min: 100 ¦ ≥ 100 N/15mm — critical for VFFS and auto-pack lines | Every Lot | QC Lab |
| L1 | Blocking Resistance | ASTM D3354 | Pass/Fail | No blocking after 24h at 40°C / 1 kg load. Lacquer must not self-adhere in roll | Every Lot | QC Lab |
| L1 | Adhesion to Target Substrate | Cross-hatch tape pull / ISO 2409 | Pass/Fail | Apply to BOPP/PET, cure 24h, cross-hatch + tape: ≥ 95% retention required | Every Lot | QC Lab |
| L1 | CoA Verification | vs. Supplier CoA | Pass/Fail | Viscosity, solids, SIT range — all within declared tolerances | Every Lot | QC Technician |
| COND | ▶ [WB] pH | pH meter | pH | 6.5 – 8.5 ¦ [WATER-BASED ONLY] pH 6.5–8.5. Out of range = coating instability and surface defects | Every Lot | QC Lab |

16. TAPES

Flexo Plate Mounting Tape (TESA / 3M / Lohman) & Web Splicing Tape

9 Level 1 tests  |  1 Level 2 tests  |  10 total

Product code match is MANDATORY — tape hardness (Shore OO) determines print quality. Wrong grade = immediate and recurring print pressure inconsistency across all jobs.

| LV | TEST NAME | METHOD | UNIT | SPEC / LIMIT & NOTES | FREQUENCY | TESTED BY |
| --- | --- | --- | --- | --- | --- | --- |
| L1 | Product Code / Part Number Match | vs. Purchase Order | Pass/Fail | TESA/3M/Lohman part number on tape MUST match PO exactly. Wrong hardness = REJECT | Every Roll | Operator |
| L1 | Visual — Liner and Foam Condition | Visual | — | Liner undamaged, no adhesive bleed, no exposed adhesive, no foam delamination | Every Roll | Operator |
| L1 | Width | Vernier caliper | mm | Within ±0.5 mm of declared width (19 mm / 25 mm / per spec) | Every Roll | Operator |
| L1 | Core Inner Diameter | Vernier caliper | mm | 76 mm ± 1 mm — must fit mounting equipment mandrel exactly | Every Roll | Operator |
| COND | ▶ [MOUNTING] Foam Thickness | Micrometer — 3-point | mm | [MOUNTING TAPE] Within ±0.05 mm of nominal TDS value. Controls print impression depth | Every Lot (2 rolls) | QC Technician |
| COND | ▶ [MOUNTING] Compressibility / Hardness | Shore OO Durometer / ASTM D2240 | Shore OO | [MOUNTING TAPE] Verify hardness grade matches print application spec per TDS | Every Lot | QC Technician |
| L1 | Peel Adhesion | ASTM D1000 — 180° peel | N/25mm | Min: 10 ¦ ≥ 10 N/25mm — holds plate at full press speed and impression pressure | Every Lot | QC Technician |
| COND | ▶ [SPLICE] Splice Type Compatibility | vs. Press specification | Pass/Fail | [SPLICING TAPE] Confirm: flying splice or butt splice — press-tested | Every Lot | QC Technician |
| L1 | CoA / TDS Match | vs. Supplier TDS | Pass/Fail | Thickness, hardness, peel — all per TDS confirmed | Every Lot | QC Technician |
| L2 | Solvent Resistance | 30-min immersion in ethyl acetate | — | No foam swelling or adhesive failure after 30 min. Press solvent exposure check | Quarterly | QC Lab |

17. PACKING MATERIALS

Corrugated Cartons / Paper Cores & Tubes / Pallets (Wood & Plastic) / Buckets

13 Level 1 tests  |  2 Level 2 tests  |  15 total

ISPM-15 phytosanitary stamp on wooden pallets is MANDATORY for import compliance — a missing stamp can hold an entire container at customs. Check every pallet, every stringer.

| LV | TEST NAME | METHOD | UNIT | SPEC / LIMIT & NOTES | FREQUENCY | TESTED BY |
| --- | --- | --- | --- | --- | --- | --- |
| L1 | Visual — Condition on Arrival | Visual | — | No crush damage, moisture staining, delamination, puncture or contamination | Every Pallet | Operator |
| L1 | Quantity / Count Verification | Physical count | pcs | Actual count vs. delivery note. Short delivery = partial acceptance with notation | Every Delivery | Operator |
| L1 | Label / Grade Match vs. PO | vs. Purchase Order | Pass/Fail | Confirm grade, dimensions and supplier code on label match PO | Every Lot | Operator |
| COND | ▶ [CARTON] Dimensions L×W×H | Steel tape / caliper | mm | [CARTON] All three dimensions within ±3 mm of PO spec. Sample 5 pcs per lot | Every Lot (5 pcs) | QC Technician |
| COND | ▶ [CARTON] Ply and Flute Verification | Visual cross-section | — | [CARTON] Verify ply count (3 or 5) and flute type (B/C/BC) match order. Wrong ply = compression failure | Every Lot | QC Technician |
| COND | ▶ [CORE] Inner Diameter (ID) | Vernier caliper — 3-point | mm | [CORE] ID within ±0.3 mm. 76 mm or 152 mm standard. Wrong ID = winder crash | Every Lot (5 pcs) | QC Technician |
| COND | ▶ [CORE] Outer Diameter (OD) | Vernier caliper — 3-point | mm | [CORE] OD within ±0.5 mm — affects winding tension and core hardness | Every Lot (5 pcs) | QC Technician |
| COND | ▶ [CORE] Wall Thickness | Caliper — 4-point | mm | [CORE] Within ±0.3 mm. Thin wall = core collapse under winding tension | Every Lot (5 pcs) | QC Technician |
| COND | ▶ [CORE] Length | Steel tape | mm | [CORE] Within ±2 mm of order specification | Every Lot (5 pcs) | QC Technician |
| COND | ▶ [PALLET] Dimensions | Steel tape | mm | [PALLET] L×W within ±10 mm. Height within ±5 mm | Every Lot (3 pcs) | QC Technician |
| COND | ▶ [WOOD PALLET] ISPM-15 Stamp | Visual — all 4 stringers | Pass/Fail | [WOODEN PALLET] ISPM-15 stamp MANDATORY on all 4 stringers. Missing = REJECT shipment | Every Pallet | Operator |
| COND | ▶ [PALLET] Structural Integrity | Physical inspection | Pass/Fail | [PALLET] No broken boards, stringer cracks, nail protrusion, rot or fork damage | Every Pallet | Operator |
| COND | ▶ [BUCKET] Volume and Lid Seal | Volume test / lid press | Pass/Fail | [BUCKET] Correct litre volume. Lid seats and seals correctly. No warping or leaks | Every Lot (5 pcs) | QC Technician |
| COND | ▶ [CARTON] Box Compression (BCT) | ASTM D642 | kgf | [CARTON] Per TDS — test during supplier qualification or stacking damage investigation | Supplier Qualification | QC Lab |
| COND | ▶ [CORE] Radial Crush Resistance | TAPPI T824 | N/mm | [CORE] Per TDS — qualification only or if core collapse occurs in production | Supplier Qualification | QC Lab |